Thin Film Solar Cell

A thin film solar cell (TFSC), also called a thin film photovoltaic cell (TFPV), is a solar cell that is made by depositing one or more thin layers (thin film) of photovoltaic material on a substrate. The thickness range of such a layer is wide and varies from a few nanometers to tens of micrometers. Many different photovoltaic materials are deposited with various deposition methods on a variety of substrates. Thin-film solar cells are usually categorized according to the photovoltaic material used:

- Amorphous silicon (a-Si) and other thin-film silicon (TF-Si)

- Cadmium telluride (CdTe)

- Copper indium gallium selenide (CIS or CIGS)

- Dye-sensitized solar cell (DSC) and other organic solar cells

Thin-film silicon Solar Cell

A silicon thin-film cell uses amorphous (a-Si or a-Si:H), protocrystalline, nanocrystalline (nc-Si or nc-Si:H) or black silicon. Thin-film silicon is opposed to wafer (or bulk[disambiguation needed]) silicon (monocrystalline or polycrystalline). The silicon is mainly deposited by chemical vapor deposition, typically plasma-enhanced (PE-CVD), from silane gas and hydrogen gas. Other deposition techniques being investigated include sputtering and hot wire techniques.The silicon is deposited on glass, plastic or metal which has been coated with a layer of transparent conducting oxide (TCO). A p-i-n structure is usually used, as opposed to an n-i-p structure. This is because the mobility of electrons in a-Si:H is roughly 1 or 2 orders of magnitude larger than that of holes, and thus the collection rate of electrons moving from the n- to p-type contact is better than holes moving from p- to n-type contact. Therefore, the p-type layer should be placed at the top where the light intensity is stronger, so that the majority of the charge carriers crossing the junction would be electrons. Micromorphous silicon Micromorphous silicon module technology combines two different types of silicon, amorphous and microcrystalline, in a top and a bottom photovoltaic cell. These two materials are chosen because their different absorption spectrums and easily combined process. Because the two different materials are both Si, they can be manufactured in the same technology, which now is PECVD. The band gap of a-Si is 1.7 eV and that of c-Si is 1.1 eV, which eventually broaden the spectral acceptance of the micromorph tandem solar cell. The c-Si layer can help to absorb the energy of red and infrared spectrum and increase the overall efficiency. The best efficiency can be achieved at transition between a-Si and c-Si. Use of protocrystalline silicon for the intrinsic layer has shown to optimize the open-circuit voltage of an a-Si photovoltaic cell.

Efficency

These types of silicon present dangling and twisted bonds, which results in deep defects (energy levels in the bandgap) as well as deformation of the valence and conduction bands (band tails). The solar cells made from these materials tend to have lower energy conversion efficiency than bulk silicon (also called crystalline or wafer silicon), but are also less expensive to produce. The quantum efficiency of thin-film solar cells is also lower due to reduced number of collected charge carriers per incident photon. Amorphous silicon has a higher bandgap (1.7 eV) than crystalline silicon (c-Si, 1.1 eV), which means it absorbs the visible part of the solar spectrum more strongly than the infrared portion of the spectrum. As nc-Si has about the same bandgap as c-Si, the nc-Si and a-Si can advantageously be combined in thin layers, creating a layered cell called a tandem cell. The top cell in a-Si absorbs the visible light and leaves the infrared part of the spectrum for the bottom cell in nc-Si. Recently, solutions to overcome the limitations of thin-film silicon have been developed. Light trapping schemes where the incoming light is obliquely coupled into the silicon and the light traverses the film several times enhance the absorption of sunlight in the films. Thermal processing techniques enhance the crystallinity of the silicon and pacify electronic defects.

Commercial Uses

First Solar, the CdTe thin-film manufacturer stated that "at the end of 2007, over 300 MW of First Solar PV modules had been installed worldwide." Below is a list of several recent installations:

Since 16 October 2008, Germany's largest thin-film pitched roof system, constructed by Riedel Recycling, has been in operation and producing solar power in Moers near Duisburg. Over eleven thousand cadmium telluride modules, from First Solar, deliver a total of 837 kW.

First Solar recently completed a 2.4 MW rooftop installation as part of Southern California Edison program to install 250 MW of rooftop solar panels throughout Southern California over by 2013.

First Solar announced a 7.5 MW system to be installed in Blythe, CA, where the California Public Utilities Commission has accepted a 12 ¢/kWh power purchase agreement with First Solar (after the application of all incentives).

Construction of a 10 MW plant in the Nevada desert began in July 2008. First Solar is partnering with Sempra Generation, which will own and operate the PV power-plant, being built next to their natural gas plant.

Stadtwerke Trier (SWT) in Trier, Germany is expected to produce over 9 GWh annually

A 40 MW system is being installed by Juwi in Waldpolenz Solar Park, Germany. At the time of its announcement, it was both the largest planned and lowest cost PV system in the world. The price of 3.25 euros translated then (when the euro was equal to US$1.3) to $4.2 per installed watt.4.8KW of thin film flexible solar panels manufactured by Uni-Solar Ovonic installed on a South Beach hurricane-prone residence in 2008. Denver-based Conergy Americas and officials at California's South San Joaquin Irrigation District (SSJID)[20] have installed what is believed to be the world's first single-axis solar tracking system featuring thin-film photovoltaic cells.